Supporting Information:

Rapid naked eye detection of arginine by pomegranate peel extract stabilized gold nanoparticles

Table of content

- UV-vis absorption spectra, TEM and SAED images of pomegranate peel extract stabilized AuNPs synthesized at different concentrations of HAuCl4 (10-2 to 10-5 M).

- UV-vis absorption spectra of AuNP1 and AuNP2 with the addition of different amino acids.

- UV-vis absorption spectra of AuNP3 and AuNP4 with the addition of different amino acids.

- The plot of A650/ A527 vs the concentration of arginine.

- Table: Zeta potential of amino acids and with the addition of AuNPs.

- DLS measurement of AuNPs with the addition of arginine.

- EDAX pattern and mapping of AuNP2 + arginine system.

- FT-IR spectrum of a) pomegranate peel extract b) arginine (10-3 M) and c) pomegranate peel extract stabilized AuNP2 + arginine (10-3 M).

- Interference study of AuNP1 + arginine, AuNP3 + arginine and AuNP4 + arginine in presence of other amino acids.

- UV-vis absorption spectra of extract, arginine and extract + arginine.

- Table S2: Comparison of present work with the reported methods for the colorimetric detection of arginine (Arg).

Fig. S1. a) UV-vis absorption spectra, the corresponding photographic image (bottom panel) of pomegranate peel extract stabilized AuNPs synthesized at different concentrations of HAuCl4 (10-2 to 10-5 M) (The as-synthesized AuNPs are represented as: AuNP1 (10-2 M), AuNP2 (10-3 M), AuNP3 (10-4 M) and AuNP4 (10-5 M)) and TEM images of b) AuNP1, c) AuNP2, d) AuNP3 and e) AuNP4. Insets are the corresponding SAED (b-e) images.

Fig. S2. UV-vis spectra of the a) AuNP1 and b) AuNP2, upon addition of different amino acids (10-2 M) and (bottom panel) corresponding photographic images.

Fig. S3. UV-vis spectra of the a) AuNP3 and b) AuNP4, upon addition of different amino acids (10-2 M) and (bottom panel) corresponding photographic images.

Fig. S4. The plot of A650/ A527 vs the concentration of arginine (the error bares illustrate the standard deviation from three independent measurements).

Table S1 Zeta potential of different amino acids (10-2 M) in distilled water and with the addition of AuNP1, AuNP2, AuNP3 and AuNP4.

| S. NO | Amino acids (AA) [10-2 M] | Zeta potential (eV) |  | Zeta potential of AA+AuNP1 (eV) | Zeta potential of AA+AuNP2 (eV) |  | Zeta potential of AA+AuNP3 (eV) |  | Zeta potential of AA+AuNP4 (eV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | L-Ala | -14.40 |  | -17.85 | -25.20 |  | -22.05 |  | -22.25 |
| 2 | Β-Ala | -16.50 |  | -23.00 | -26.40 |  | -23.20 |  | -22.15 |
| 3 | Dl-Ala | -15.90 |  | -21.30 | -23.90 |  | -21.60 |  | -22.15 |
| 4 | Cys | -12.20 |  | -21.45 | -21.40 |  | -24.80 |  | -24.15 |
| 5 | Asp | -3.90 |  | -19.00 | -24.20 |  | -19.00 |  | -20.45 |
| 6 | Glu | -5.70 |  | -21.75 | -21.80 |  | -20.45 |  | -22.85 |
| 7 | Phe | -19.90 |  | -20.25 | -23.80 |  | -20.45 |  | -21.85 |
| 8 | His | -12.30 |  | -17.20 | -20.14 |  | -17.25 |  | -18.25 |
| 9 | IIe | -20.80 |  | -19.15 | -23.30 |  | -20.80 |  | -22.65 |
| 10 | Lys | -9.40 |  | -16.80 | -20.04 |  | -17.80 |  | -17.75 |
| 11 | Leu | -16.90 |  | -20.95 | -22.25 |  | -21.15 |  | -23.75 |
| 12 | Met | -13.70 |  | -21.50 | -21.55 |  | -22.25 |  | -23.25 |
| 13 | Asn | -1.027 |  | -19.95 | -24.90 |  | -26.60 |  | -23.95 |
| 14 | Pro | -16.80 |  | -20.50 | -26.05 |  | -18.80 |  | -27.10 |
| 15 | Gln | -11.50 |  | -22.45 | -21.95 |  | -21.15 |  | -19.55 |
| 16 | Arg | -26.10 |  | -11.46 | -12.65 |  | -12.46 |  | -9.65 |
| 17 | Ser | -13.60 |  | -19.45 | -22.05 |  | -20.10 |  | -21.65 |
| 18 | Thr | -17.30 |  | -19.20 | -20.80 |  | -23.00 |  | -22.50 |
| 19 | Val | -14.70 |  | -23.35 | -21.50 |  | -21.01 |  | -20.95 |
| 20 | Trp | -16.60 |  | -23.75 | -21.05 |  | -19.65 |  | -23.45 |
| 21 | Tyr | -20.10 |  | -22.15 | -21.40 |  | -19.30 |  | -21.15 |
| 22 | Ornithine | -1.02 | -16.95 |  | -20.35 | -17.30 |  | -17.45 |  |
| 23 | Gly | -17.08 | -19.00 |  | -20.34 | -20.05 |  | -21.02 |  |

Fig. S5. Change in the particle size of AuNPs (1-4) upon addition of arginine by dynamic light scattering measurement.

Fig S6. FT-IR spectrum of a) pomegranate peel extract b) arginine (10-3 M) and c) pomegranate peel extract stabilized AuNP2 + arginine (10-3 M).

Fig. S7. a) EDAX pattern, b) STEM image of AuNP2 + arginine system [10-4 M], elemental mapping shows the presence of c) Au and d) N in the system.

Fig. S8. Interference study of a) AuNP1 + arginine b) AuNP3 + arginine and c) AuNP4 + arginine in the presence of other amino acid (10-2 M).

Fig. S9. UV-vis absorption spectra of extract, arginine (10-2 M-200 µL) and extract + arginine. Inset shows the corresponding photographs.

Table S2: Comparsion of present work with the reported methods for the colorimetric detection of arginine (Arg).

| Reducing and stabilizing agent | Reaction condition | Detection range | References |
| --- | --- | --- | --- |
| Sodium citrate dihydrate | ~ 100̊ C | 0.08-13.2 µM | 18 |
| Quercetin and NaOH | Room temperature | 2.5–1,250 μM | 19 |
| 4-Amino nicotinic acid | Heating at 100̊ C | 0.001-100 µM | 21 |
| Pomegranate peel extract | Room temperature | 1µM-0.1M | Our work |