Electronic supplementary information for:

**Nitrogen-doped carbon quantum dots (N-CQDs)/Co3O4 nanocomposite for high performance supercapacitor**

Mu. Naushada, **b**\*, Tansir Ahamada, Mohd Ubaidullaha\*, Jahangeer Ahmeda, Ayman A. Ghafara, Khalid M. Al-Sheetana and Prabhakarn Arunachalamc

aDepartment of Chemistry, College of Science, King Saud University, 11451 Riyadh, Saudi Arabia

bYonsei Frontier Lab, Yonsei University, Seoul, Korea

cElectrochemical Sciences Research Chair (ESRC), Chemistry Department, College of Science, P.O. Box 2455, King Saud University, Riyadh 11451, Saudi Arabia

E-mail: [mtayyab@ksu.edu.sa](mailto:mtayyab@ksu.edu.sa) (Mohd Ubaidullah); [mnaushad@ksu.edu.sa](mailto:mnaushad@ksu.edu.sa) (Mu. Naushad)

**SUMMARY:**

**S-1:** *Characterization techniques used*

**S-2:** *Fabrication of electrode*

**S: 3** *High resolution XPS spectrum of O1s*

**S: 4***Charge storage mechanisms*

**S-1: *Characterization******techniques used***

The surface texture and morphological details were examined by field emission-scanning electron microscopy (JEOL, JSM- 6701F), scanning electron microscopy (SEM; Hitachi S-7400), and transmission electron microscopy (JEOL, JEM-2010). The X-ray diffraction (XRD) patterns were recorded with a Rigaku X-ray diffractometer equipped with a Cu sealed tube (λ = n1.54056 Å). The surface chemical composition was measured by Xray photoelectron spectroscopy (XPS). The N2 sorption isotherms were measured by a Micromeritics ASAP 2420 system. Electrochemical experiments in a three-electrode cell were executed in 6 M aqueous KOH with Ag/AgCl as reference electrode and platinum wire as a counter electrode. Cyclic voltammetry (CV) was measured from −0.4 to +0.6 V. Galvanostatic charge−discharge (GCD) was measured in between −0.4 and 0.6 V. Electrochemical impedance spectroscopy (EIS) was run at 5 mV amplitude between 100 kHz and 0.01 Hz in an open circuit. The electrochemical parameters were calculated using standard equations

**S-2: Fabrication of electrode:**

Tofabricate the electrode, a slurry of N-CQDs/Co3O4 nanocompositepowder was mixed in ethanol and then few drops poly-vinylene difluoride (PVDF) were intimately mixed in N-methyl-2-pyrrolidinone (NMP, showa). This slurry was painted onto a piece (1x1 cm2) of nickel foam and dried in oven at 60°C for 10 hrs.

**S-3: High resolution XPS spectrum of O1s:**



**S-4: Charge storage mechanism:**

The mechanism of electrochemical reaction can be expressed as follows;

Co3O4 + OH− + H2O **⇔** 3CoOOH + e−

CoOOH + OH− **⇔** CoO2 + H2O + e–