Chemical Depolymerization of Recycled PET to Oxadiazole and Hydrazone Derivatives: Synthesis, Characterization, Molecular Docking and DFT study

Nazia Tarannum1,* Rizwan Khan1, Shoaiba Ansari1, Ranu Agrawal2, Swapnil Mishra3, Mohd Ubaidullah4, Abdulla A. Al-Kahtani4

1Department of Chemistry, Chaudhary Charan Singh University Meerut, Uttar Pradesh, India-250005

2Department of applied science, SCRIET, Chaudhary Charan Singh University Meerut, Uttar Pradesh, India-250005

3Centre for Bioinformatics, Allahabad University, Allahabad, Uttar Pradesh, India-211002

4Department of Chemistry, College of Science, King Saud University, Riyadh 11451, Saudi Arabia Corresponding author: naz1012@gmail.com

Figure S1: General and synthesized structure of oxadiazole and hydrazone derivatives

Figure S2: FTIR spectra of oxadiazole derivatives (OCB and OHB)

Figure S3: FTIR spectra of hydrazone derivatives (TCA, TBA and THD)

Figure S4: 1H NMR and 13C NMR spectra with splitting pattern and structure of OHB

Figure S5: 1H NMR and 13C NMR spectra with splitting pattern and structure of TBA and THD

Figure S6: SEM micrograph showing the internal appearance of oxadiazole derivatives (a) OCB

(b) OHB at 100X magnification

Figure S7: SEM micrograph showing the internal appearance of hydrazone derivatives (a) TCA

(b) TBA (c) THD at 500X magnification

Figure S8: Thermogravimetric (TGA/DTA) curves for oxadiazole derivatives (OCB and OHB)

Figure S9: Thermogravimetric (TGA/DTA) curves for hydrazone derivatives (TCA, TBA and

THD)

Figure S10: DSC curve for hydrazone derivatives (TCA and TBA)

Table S1: The solubility of the synthesized compounds in different solvents

| S.N. | Solvent | Compound OCB | Compound OHB | Compoud TCA | Compound TBA | Compound THD |
| --- | --- | --- | --- | --- | --- | --- |
| 01 | ### Dimethyl sulfoxide (DMSO) | × | Δ | × | Δ | Δ |
| 02 | Distilled water | × | × | × | × | × |
| 03 | Benzene (C6H6) | × | × | × | × | × |
| 04 | Chloroform (CHCl3) | ÷ | × | × | ÷ | ÷ |
| 05 | ### Tetrahydrofuran (THF) | × | × | × | × | × |
| 06 | Methanol (CH3OH) | × | × | × | × | × |
| 07 | Carbon tetrachloride (CCl4) | × | Δ | × | × | ÷ |
| 08 | Carbon disulphide (CS2) | × | × | × | × | × |
| 09 | Acetonitrile (CH3CN) | × | × | × | × | × |
| 10 | Dioxane (C4H8O2) | × | × | × | × | × |
| 11 | Benzyl alcohol (C6H5CH2OH) | × | × | × | × | × |
| 12 | 0.1 NH4Cl | × | × | × | × | × |
| 13 | Toulene (C7H8) | × | × | × | × | × |
| 14 | Acetic acid (CH3COOH) | × | × | × | × | × |
| 15 | Acetone (30%) + Methanol (20%) | × | × | × | × | × |
| 16 | Dimethylformamide (DMF) | × | × | × | ÷ | × |
| 17 | Triflouro -acetic acid (CF3COOH) | Δ | ÷ | Δ | Ʃ | Δ |
| 18 | Acetone (C3H6O) | × | × | × | × | × |

Note: Not Soluble: ×, Partially Soluble: ÷, Soluble on heating: Δ, Soluble at room temperature: Ʃ

Table S2: Comparison of the theoretical and experimental elemental analysis results of the synthesized compounds

OCB: 1,4-bis(5-(2-chlorophenyl)-1,3,4-oxadiazole-2-yl)benzene. OHB: 1,4-bis(5-(4-hydroxyphenyl)-1,3,4-oxadiazole-2-yl)benzene. TCA: N,N′-bis(2-chlorobenzylidene)terephthalo hydrazide. TBA: N,N′-bis(benzylidene)terephthalohydrazide.THD: N,N′-bis(4-hydroxybenzylidene)-terephthalo hydrazide

| Compounds | Experimental elemental analyses |  |  |  | Theoretical elemental analyses |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | C% | H% | N% | S% | C% | H% | N% | S% |
| OCB | 67.50 | 2.35 | 12.29 | - | 66.68 | 2.75 | 12.85 | - |
| OHB | 65.85 | 3.68 | 14.17 | - | 66.33 | 3.51 | 14.07 | - |
| TCA | 60.28 | 4.41 | 12.58 | - | 60.13 | 4.10 | 12.75 | - |
| TBA | 70.56 | 4.61 | 15.20 | - | 71.35 | 4.86 | 15.13 | - |
| THD | 65.92 | 5.04 | 13.44 | - | 65.67 | 4.47 | 13.90 | - |

Table S3: Thermodynamic parameters of the compounds, as obtained by the DFT study in the ground state

|  | OHB | OCB | TBA | TCA | THD |
| --- | --- | --- | --- | --- | --- |
| E (Thermal) kcal/Mol | 210.381 | 194.338 | 232.676 | 218.352 | 236.694 |
| Cv Cal/Mol-Kelvin | 84.984 | 83.790 | 82.939 | 83.715 | 91.356 |
| S Cal/Mol-Kelvin | 150.916 | 150.819 | 153.454 | 152.946 | 167.307 |
| Degree of freedom | 126 | 120 | 132 | 132 | 138 |
| Full point group | C1 | C1 | C1 | C1 | C1 |
| Dipole Moment (Debye) | 4.9268 | 3.8776 | 3.1281 | 3.7645 |  |
| ZPVE kcal/Mol | 197.4787 | 181.491 | 219.700 | 204.3433 | 222.1189 |

Table S4: Supplementary data of vibrational frequencies (cm-1) of the synthesized compounds

| Vibrational Frequencies (cm-1) | OCB | OHB | TBA | TCA | THD |
| --- | --- | --- | --- | --- | --- |
| 1. | 3038.4404 | 3288.1216 | 3263.1879 |  |  |
| 2. | 3042.9261 | 3861.8489 | 3256.5914 | 3651.9328 |  |
| 3. | 3042.1100 | 3861.9083 | 3040.7485 | 3654.8259 | 3860.2593 |
| 4. | 3031.7386 | 3037.9008 | 3030.2975 | 3095.0172 | 3841.4275 |
| 5 | 3032.0784 | 3039.3012 | 3029.6343 | 3042.1494 | 3644.7226 |
| 6. | 3035.4677 | 3032.3055 | 3020.8269 | 3039.8454 | 3240.4879 |
| 7. | 3019.2926 | 3020.6696 | 3010.6425 | 3028.7881 | 3283.8167 |
| 8. | 3021.2973 | 3011.7172 | 1655.6963 | 3008.8437 | 3039.4463 |
| 9. | 3021.7074 | 1655.7158 | 1652.5055 | 2694.3841 | 3027.9525 |
| 10. | 3010.2722 | 1655.2740 | 1640.1672 | 1842.0610 | 3033.1470 |
| 11. | 3017.2027 | 1638.4451 | 1616.4104 | 1650.8289 | 1655.3055 |
| 12. | 1638.3552 | 1555.4011 | 1550.0296 | 1633.0806 | 1639.0234 |
| 13. | 1626.9457 | 1563.3004 | 1555.3714 | 1622.0985 | 1563.9511 |
| 14. | 1533.7883 | 1467.7462 | 1424.5083 | 1574.4694 | 1509.9535 |
| 15. | 1336.9622 | 1402.5961 | 1454.3763 | 1539.2395 | 1522.2784 |
| 16. | 1286.0117 | 1287.9669 | 1511.7743 | 1516.4344 | 1459.3684 |
| 17. | 1179.7743 | 1326.0494 | 1408.4559 | 1523.1317 | 1445.3199 |
| 18. | 1161.4761 | 1168.3421 | 1376.3362 | 1466.5925 | 1375.6214 |
| 19. | 1143.6211 | 1217.5004 | 1217.0417 | 1453.5016 | 1342.8486 |
| 20. |  | 1163.9387 | 1189.3491 | 1377.8349 | 1232.8912 |
| 21. |  | 1123.1972 | 1174.1145 | 1320.8984 | 1207.2488 |
| 22. |  | 1124.8094 | 1167.7175 | 1209.7135 | 1118.7722 |
| 23. |  | 1083.5551 | 1090.5790 | 1173.5037 | 1104.7058 |
| 24. |  | 1011.7182 | 1072.1880 | 1163.8807 1172.7698 1093.2783 1087.5121 | 1045.4853 |

Table S5: Molecular docking results of the five ligands with GlcN-6-P (PDB: 1jxa).

| Compounds | BE (kcal/Mol) | Number of formed hydrogen bonds | H Bond distance (Å) | Residues involved in the formation of the hydrogen bonds with their respective distances |
| --- | --- | --- | --- | --- |
| OCB | −6.82 | 1 | 2.738 | Thr302 |
| OHB | −4.48 | 1 | 2.813 | Ser604 |
| TCA | −7.04 | 2 | 3.040, 3.066 | Gln348, Ser349 |
| TBA | −6.34 | 2 | 2.834, 3.148 | Gln348, Ser349 |
| THD | −8.30 | 3 | 3.230, 2.870, 3.30 | Thr302, Ser401, Ala602 |
| Voriconazole | −7.03 | Nil | - | - |

Table S6: Molecular docking results of the five ligands, along with voriconazole with CYP51B(PDB:4uyl)

| Compound | BE (kcal/Mol) | Number of formed hydrogen bonds | Hydrogen Bond distance (Å) | Residues involved in the formation of the hydrogen bonds with their respective distances |
| --- | --- | --- | --- | --- |
| OCB | −11.96 | 1 | 2.738 | Thr302 |
| OHB | −11.55 | 1 | 2.813 | Ser604 |
| TCA | −11.88 | 1 | 2.768 | His310 |
| TBA | −10.21 | 2 | 2.791, 2.984 | His310, Ala303 |
| THD | −9.35 | 2 | 2.693, 2.828 | Thy136, Ala303 |
| Voriconazole | −8.12 | 1 | 3.099 | His310 |